|  |  |  |  |
| --- | --- | --- | --- |
| **Specie** | **NFPA – fire rating** | **Janka Hardness Rating** | **Average Weight** |
| Ipe (ee-pay) | A (the same as concrete) | 3680 | 72 lbs./cu. ft. |
| Cumaru | A | 3540 | 67 lbs./cu. ft. |
| Massaranduba (massa) | A | 3190 | 66 lbs./cu. ft. |
| Garapa | A | 1700 | 50 lbs./cu. ft. |
| Cypress | C | 570 | 32 lbs./cu. ft. |
| Inland Red Cedar | B | 350 | 23 lbs./cu. ft. |
| Atlantic White Cedar | B | 350 | 24 lbs./cu. ft. |
| Red Oak | C | 1260 | 45 lbs./cu. ft. |
| White Oak | C | 1360 | 50 lbs./cu. ft. |
| Heart Pine |  | 1225 |  |

NFPA is the National Fire Protection

The Janka rating is a measure of the amount of force required to push a .444" diameter steel ball half way into a piece of wood.

**Wood Haven, Inc.** [**www.rainscreenclip.com**](http://www.rainscreenclip.com)[**www.deckclip.com**](http://www.deckclip.com) **1-800-545-8884**